## Slide 1: Plasma Polish
Dry Polish Solution to Prepare Epi-Ready SiC for Power Applications
Amandev Singh Product Manager Oxford Instruments Plasma Technology

## Slide 2: Outline
Company Overview
+
Plasma Polish – A Game Changer
+
Plasma Polish – Customer Value Proposition
+
Program Update and conclusions
+
1

## Slide 3: Company Overview

## Slide 4: Oxford Instruments Plasma Technology
3
Research & Discovery
Materials & Characterisation
8 business units supporting all areas of semiconductor manufacturing and research
ANDOR
Development & manufacture of high performance scientific digital cameras and light microscopes
MAGNETIC RESONANCE
Offering a range of benchtop Nuclear Magnetic Resonance (NMR) instruments
NANOSCIENCE
Enabling quantum technologies, nano technology research, advanced materials & nano device development
Products and solutions that enable the fabrication and characterisation of devices down to the atomic scale.
Provides advanced solutions that create unique environments and enable imaging and analytical measurements down to molecular and atomic levels.
X-RAY TECHNOLOGY
Leading manufacturer of x-ray tubes, power supplies & integrated x-ray sources
NANOANALYSIS
Enabling materials characterisation and sample manipulation at the nanometre scale
ASYLUM
Leader in development & manufacture of Atomic Force Microscopy (AFMs)
PLASMA TECHNOLOGY
Leading provider of etch and deposition processing solutions and recipes
WITec
Leader in d Raman, Atomic Force Microscopy, and Scanning Near-field Optical Microscopy

## Slide 5: Active in all Compound Semiconductors Markets
4
GaN Power/RF
Datacom
SiC Power
Quantum
Augmented Realty
3D Sensing
Quantum technology solves complex problems such as traffic flow and enables secure communications
SiC devices enables more efficient power conversion in electric vehicles & renewable energy.
Augmented reality has applications in advan-ced health care and consumer electronics.
3D sensing using GaAs based VCSELs enables autonomous machines, e.g. vehicles.
GaN devices for 5G/6G base stations and power efficient consumer electronics.
Next generation InP/ GaAs based lasers and receivers increase optical fibre data bandwidth.
5G
6G

## Slide 6: Plasma Polish – A Game Changer
Stable, cost effective and green Polish solution
to prepare epi-ready SiC substrate surface

## Slide 7: Why Polish ? Need Damage free crystal for Front End Manufacturing
6
Other
Deposition
Etch
EPI
Polish
Grinding
Slicing
Flat for-mation
Crystal Growth
Substrate Manufacturing
Front End Manufacturing
Grind
Polish
Hsieh, C.-H.; Chang, C.-Y.; Hsiao, Y.-K.; Chen, C.-C.A.; Tu, C.-C.; Kuo, H.-C. Recent Advances In Silicon Carbide Chemical Mechanical Polishing Technologies. Micromachines 2022, 13, 1752.
Why Polish: To get good crystal surface to grow Epi.
  No sub-surface damage or contaminants.
  Means: Remove all defective material /nano-particles left by slicing/ grinding
  In Practice: CMP by design only targets surface/roughness.

## Slide 8: Plasma Polish
7
An etch process to provide epi-ready surface in SiC substrate production
Proprietary process (patent pending)
Based on proven PlasmaPro 100 Cobra single wafer etch system with modified hardware
smooth / epi-ready surface
free of subsurface damage
reliable and consistent surface quality
low operating cost
clean process (standard process gas / abatement)
proven with SiC pin-Diodes and MOSFETs
Crystal growth
Slicing and grinding
EPI
Device
Plasma Polish
PlasmaPro 100 Cobra single wafer etch system

## Slide 9: How the process works: Surface-level concept Plasma Polish is an etch process directly targeting subsurface damage
8
Fine Grinding
Subsurface Damage: Dense Network of Narrow Scratches and defects induced by grinding.
Ra (nm) – 1.50
10x10µm2
Plasma Polish
CMP
Preferential etching of damaged area.
Effectively leaving behind good crystal structure and approx. 50% Ra reduction.
Removing Top Surface Sequentially.
Chemical and Mechanical actions to achieve high flat-ness.
10x10µm2
Ra (nm) – 0.70
Subsurface damage free surface with some leftover waviness
Highly flat surface with a likely-hood of observing leftover subsurface damage

## Slide 10: Process Validation: Epi-Growth
9
Post Epi Roughness of Plasma Polish wafers comparable to benchmark CMP reference processed using same recipe.
Plasma Polish - Oxford Instruments
CMP Reference
Standard recipe (10um Dep)
80% Ra Reduction.
MOCVD Growth
After deposition
After deposition
Plasma Polish
Ra (nm) – 0.70
Ra (nm) – 0.14
Ra (nm) – 0.12

## Slide 11: Device Validation – MPD & MOSFETs
10
SiC Epi growth
Plasma Polish & CMP Substrates (Wolfspeed)
Optical/PL Inspection
MPD/MOSFETS
150mm Wafers - Wolfspeed
Plasma Polish ↔ Chemical and Mechanical Polish (CMP)
Merged pin Diodes (MPD) operating at 1200V and 10 A and dies area of 2.4x2.4mm2
Comparison between 2 CMP and 2 Plasma Polish wafers
MOSFETS operating at 80m, 1200V and a dies area of 2.83x2.83 mm2
Comparison between 3 CMP wafers and 3 Plasma Polish wafers

## Slide 12: Device Validation – Merged pin Diodes Yields
11
Sub-surface damage and it’s yield impact observed in a production grade substrate supplied by a leading supplier
92% Dies passed
93% Dies passed
97% Dies passed
97% Dies passed
94% Dies passed
89% Dies passed
97% Dies passed
91% Dies passed
Plasma Polish
CMP REFERENCE
VB at 500µA
(VB>1500V)
JR at 600V
(JR < 1.7E-6 A/cm2)
Sub-surface damage remains after CMP revealed at epi (not seen prior)

## Slide 13: Device Validation – MOSFETs Yields
12
Average Pass rates/ Good Devices, (%)
3 Plasma Polish wafers ↔ 3 CMP wafers
MOSFETs operating at 1200V
Plots reporting the average of the % of dies passed/wafer
MOSFETs on Plasma Polish substrates perform at same level as MOSFETs on CMP substrates

## Slide 14: Plasma Polish – Value Proposition
Cost reduction
Potential Yield improvement
Environment friendly

## Slide 15: Benefits of the Plasma Polish process
1. Based on average substrate costs of USD 1200/6″ wafer and 24 USD/6″ wafer savings in plasma polishing operating costs 2. Based on ~ USD 500-600/wafer for FE manufacturing
USD 23/wf
(direct cost savings)
Cost reduction for 150 mm substrates, plus additional USD 50-70/wf cost potential through thinner slicing1
Cost reduction for front-end manufacturers for each pp line yield improvement2
USD 12-15/wf
(potential cost savings)
USD 45/wf
(direct cost savings)
Cost reduction for 200 mm substrates
Crystal growth
Slicing and grin-ding
EPI
Device manufac-turing
Plasma Polish
CMP
Oxford Instruments Plasma Polish as alternative to CMP process
PlasmaPro 100 Cobra single wafer etch system
Reduction of operating costs by USD 27/wafer
Enabler for thinner wafer slicing to increase absolute numbers of wafer/boule and reduce costs
High process and results stability through replacement of mecha-nical processing
Minimization of the utilization of toxic materials
14

## Slide 16: Program Update and Conclusions

## Slide 17: Program Update
Market Launch (ICSCRM 2022)
Program Inception (2020)
Current Status
Substrates from 5 SiC customers/ partners.
Over 150 stable full wafer process runs.
Demonstrated Tool-to-Tool process transfer.
Over 20 Additional active customer engagements
Exploratory joint programs to expand use-cases
Post Launch
  Post Market Launch Engagements
Asia
EMEA
USA
16

## Slide 18: Conclusions
Oxford Instruments is the recognized partner for Plasma Technology for CS Industry
  Trusted partner in RnD and High-Volume Manufacturing.
  Established production platform supporting key processes in CS Market.
  Continuously investing in new process technology for power Applications.
    Active programs in SiC as well as GaN to support Power Semiconductors.
Plasma Polish: A powerful polishing solution for SiC substrate manufacturing
  Validated using industry standard MOSFET and MPD devices.
  Significantly Lower Cost compared to current polishing solutions.
  Offering high stability and process capability (proven independent of substrates vendors).
  Environmentally friendly process, with significantly higher ease of use.
Expanding program: Active engagement with key SiC PE customers.
17